## Slide 1: High-energy phase contrast
Why high energies?
Absorption
Phase interaction
Phase is relatively more important at higher energies
It may be possible to decrease the absorption and therefore the dose while keeping a good contrast from phase-sensitive methods.
60-160 keV

## Slide 2: High-energy phase contrast
The technical challenge
Large thickness (> 500 μm of gold) needed to block X-rays above 100 keV
Small period needed for higher sensitivity
Conventional gratings cannot be fabricated with such thickness and a small period (2.8 μm)
Edge-on illumination
Illumination from the side (edge-on) is a solution

## Slide 3: High-energy phase contrast
Two edge-on systems built at PSI
High-voltage X-ray tube: 160 kVp
Gold gratings, 2.8 μm pitch
Symmetric setup
1st Lohmann distance
Nominal energies 100 and 120 keV

## Slide 4: High-energy phase contrast Performance
120 keV
100 keV

## Slide 5: High-energy phase contrast The first images: an electronic chip at 100 keV
Complementarity of absorption and differential phase
All soldering points visible in the phase image, even under the strongly absorbing resistors

## Slide 6: High-energy phase contrast The first images: soft materials at 120 keV
Complementarity of absorption and dark field
Contrast from soft polystyrene foam increased from 2 to 20%
air
foam
steel

## Slide 7: High-energy phase contrast
The edge-on setup